# Watertight manhole cover SD5, rectangular type

# Manhole cover, watertight up to 1 m head of water, rectangular in shape, completely made of 1.4307 
(AISI 304 L) stainless steel.

Based on DIN 1239:2018-4, suitable for use in Ex zone 1.

The cover is made of stainless steel plate, with a centrally raised profile, robust external hinges, stainless steel gas assisted spring damper, integrated arrestor which can only be undone by hand, handle, circumferential rubber seal (frost-proof and weather resistant) fixed in a slot, central lock and protective hood of brass, which can only be opened with a special key.

A connection for potential equalisation is provided.

The frame consists of an angle section for bolted fixing, with two internal lift locks. Manhole cover and frame shielded arc-welded, acid treated in a pickling bath and passivated.

Fixing material, gasket strip and operating key included.

Options:

➤ 1.4404 (AISI 316 L) stainless steel

➤ Insulation of the cover, without FCKW

➤ Safety lock for increased security, with or without

➤ profile cylinder

➤ Non-standard sizes

➤ Magnetic contact

➤ Flood-proof up to 5 m head of water, with multiple screw connection 
(clear opening dimensions to be taken into account)

➤ Application in plants in contact with ozone on request

➤ Back-up proof up to 0.5 bar, with multiple screw connection (clear opening dimensions to be taken into account)

➤ Unscrewable air vent with X-piece to seal the vapour hood opening in case of danger of flood water

➤ Safety guard / barrier

➤ Safety guard / antifall guard